## Slide 1: Lithium Niobate on Insulator Integrated Photonics from Fabrication to Classical and Quantum Applications
Presenter: Aaron Danner
National University of Singapore
E-mail: adanner@nus.edu.sg
Les Houches School of Physics, France, May 12, 2025 - May 23, 2025
Ecole de Physique des Houches 149 Chemin de la Côte F-74310 Les Houches
Part 1: How LN’s structure leads to its optical properties (Thurs, May 15, 10:45 am – 12:15 pm)
Part 2: Comparison of LN to other materials
(Fri, May 16, 10:45 am – 12:15 pm)

## Slide 2: What’s in the glass?
Yes, it is a glass of lithium niobate.

## Slide 3: Birefringence in lithium niobate
Actual behavior
Just the ordinary ray

## Slide 4: Birefringence: when
CALCITE (no=1.6584 and ne=1.4864)

## Slide 5
Material | no | ne | Δn (“birefringence”)
beryl | 1.602 | 1.557 | -0.045
calcite | 1.658 | 1.486 | -0.172
calomel | 1.973 | 2.656 | 0.683
ice | 1.309 | 1.313 | 0.014
lithium niobate | 2.272 | 2.187 | -0.085
magnesium fluoride | 1.38 | 1.385 | 0.006
quartz | 1.544 | 1.553 | 0.009
ruby | 1.77 | 1.762 | -0.008
rutile | 2.616 | 2.903 | 0.287
peridot | 1.69 | 1.654 | -0.036
sapphire | 1.768 | 1.76 | -0.008
sodium nitrate | 1.587 | 1.336 | -0.251
tourmaline | 1.669 | 1.638 | -0.031
COMMON UNIAXIAL CRYSTALS

## Slide 6: In some composite materials, n < 1
Notomi et al., PRB, 62, 10696 (2000) Hoffman et al, Nature Mat., 6, 946 (2007)
GaAs rods in air (TE, d=0.7a)
InGaAs/AlInAs 80 nm, 1018 (FOM~1000)

## Slide 7: Lithium niobate vs. fruit tea
LITHIUM NIOBATE
n  2.4
FRUIT TEA
n = 1.3

## Slide 8: Lithium niobate gemstones exist
Example (May 8, 2025)
https://www.etsy.com/sg-en/listing/1496550454/lithium-niobate-square-cut-loose-faceted?ref=nla_rv-2&sts=1&logging_key=9df04a6e8f76047e403ba472406097889e4c3761%3A1496550454

## Slide 9: Positive versus negative water
NEGATIVE INDEX WATER
n = -1.33
Everything simulated in POV-Ray
Inspired by
Friedrich Lohmuller, 2013
www.f-lohmueller.de

## Slide 10
1. Lithium niobate’s crystal structure
Atomic arrangement
Physical origin of refractive index and birefringence
Physical origin of thermal expansion
Thermo-optics in lithium niobate and silicon
Physical origin of nonlinearity
2. Applications and comparison with other materials
Rotation of crystals and how that affects optics
Barium titanate – growth and fabrication
Optical computing with lithium niobate

## Slide 11: A simple cubic crystal will have isotropic properties.
Looking towards -y
Rotate by 90 degrees
“the laboratory’s coordinates”
“the crystal’s coordinates”

## Slide 12: Why is the refractive index the same when you rotate a cubic crystal to any angle?
Apply R
c
c
c
If
then
So

## Slide 13: A primitive cell of silicon: Is it really isotropic?
Looking towards +x
Rotate by 90 degrees

## Slide 14: Why silicon is still isotropic
Looking towards +x
Rotate by 90 degrees
?
AND translate by one atomic bond length

## Slide 15: Primitive unit cell of LN
+z
+z

## Slide 16: Primitive unit cell of LN
+z
+z

## Slide 17: Primitive unit cell of LN
+z
+z

## Slide 18: Primitive unit cell of LN
+z
+z

## Slide 19: Top view of lithium niobate (crystal class 3m)
120
Why is LN birefringent?

## Slide 20
Example 1(a): Light polarized along the laboratory’s -axis enters lithium niobate at a 45 angle between its and axes. Find .

## Slide 21
Example 1(b): What happens to the light?
If the light were polarized
If the light were polarized
Here, the light is polarized
Polarization dispersion
Double refraction
The two components have evolving phase shifts.

## Slide 22: Lithium niobate can be oriented along z
Li
Li
Nb
Nb
Nb
+c
Li
Li
Nb
Nb
Nb
-c

## Slide 23: Atomic motion during poling
Li+
Li+
Nb5+
Nb5+
+c
High voltage
Poled +Z
     
++++++++
Original +Z
++++++++
     
3.051 Å
3.974 Å
3.051 Å
3.974 Å
3.051 Å
3.974 Å
The negative surface oxygen layer here is more easily etched (e.g., in HF:HNO3 = 1:2) because the oxygen atoms are farther apart.
Spacings from X. Zhang et al., Materials Science and Engineering B, 120 (2005) 21-26.

## Slide 24: Periodic poling of barium titanate
50 nm
DSO
SRO
BTO
0.5 𝜇m
BTO
DSO
x
y
z
DSO
SRO
BTO
P. Aashna, H.-L. Lin, Y. Cao, Y. Yin, Y. Gao, S. S. Mohanraj, D. Zhu, A. Danner, Periodic Domain Inversion in Single Crystal Barium Titanate-on-Insulator Thin Film. Adv. Sci. 2024, 11, 2406248. https://doi.org/10.1002/advs.202406248

## Slide 25: What causes refractive index?

## Slide 26: Refractive indices of a few materials
Material | n (at 589 nm)
Air | 1.00029
Ice | 1.31
Water | 1.333
Ethyl alcohol | 1.36
Fused quartz | 1.4584
Carbon tetrachloride | 1.46
Turpentine | 1.472
Benzene | 1.501
Plexiglass | 1.51
Crown glass | 1.52
Sodium chloride | 1.544
Light flint glass | 1.58
Polystyrene | 1.59
Carbon disulfide | 1.628
Dense flint glass | 1.66
Lanthanum flint glass | 1.80
Zircon | 1.923
Diamond | 2.417
Rutile | 2.907
Gallium phosphide | 3.45
Solid sodium metal | 0.04 – i2.4
Tin | 1.5 – i5.3

## Slide 27: An empty swimming pool (air, n = 1)

## Slide 28: Water (n = +1.33)

## Slide 29: n = 0.9 (field of view near critical angle)

## Slide 30: n = -1.33

## Slide 31
n = -1.33

## Slide 32: A review of Maxwell’s variables: Free space
Electric displacement field [C/m2]
Electric field [V/m]
Permittivity of free space [ϵ0​=8.854×10−12 F/m]
Material polarization [C/m2]
Example 2(a): Free space
10V
+
-
Imagine 10V applied to a plate capacitor. The plates are 1 cm apart and they are 10 cm2 in surface area each.
  What’s the electric field E between the plates?
  What is D?
  What is the total charge on either plate?
Answers:
10 V/cm
C/cm2
C
(C=0.885 pF)

## Slide 33: A review of Maxwell’s variables: Free space
D is quite simple: How much charge is on one plate?
Example 2(b): Free space
10V
+
-
Imagine 10V applied to a plate capacitor. The plates are 1 cm apart and they are 10 20 cm2 in surface area each.
  What’s the electric field E between the plates?
  What is D?
  What is the total charge on either plate?
Electric displacement field [C/m2]
Electric field [V/m]
Permittivity of free space [ϵ0​=8.854×10−12 F/m]
Material polarization [C/m2]
Answers:
10 V/cm
C/cm2
(C=1.77 pF)
C
10 V/cm
C/cm2

## Slide 34: A review of Maxwell’s variables: Dielectric
(Same charge, less field E.)
(We kept D the same.)
Example 2(c): Fused Quartz (3.7 at DC)
2.7V
+
-
Imagine 10V 2.7 V applied to a plate capacitor. The plates are 1 cm apart and they are 10 20 cm2 in surface area each.
  What’s the electric field E between the plates?
  What is D?
  What is the total charge on either plate?
(an insulator)
(C=6.55 pF)
Electric displacement field [C/m2]
Electric field [V/m]
Permittivity of free space [ϵ0​=8.854×10−12 F/m]
Material polarization [C/m2]
Answers:
10 V/cm
C/cm2
C
C/cm2
C

## Slide 35: The situation between the plates with dielectric
WITH NO APPLIED FIELD
P = 0
WITH APPLIED FIELD
The charges are still bound, but they separated a little.
-
+
-
+
The applied voltage is the same, but the field between the plates is reduced a little, due to the charge separation there.
-
+
P > 0
Observation: Refractive index is related to charge separation.
Electric displacement field [C/m2]
P can be thought of
as “dipoles per unit volume”
= dipoles (C m) / volume (m3).

## Slide 36: Atomic forces versus force from light
How does the atomic field compare to the field from passing light?
a) In a Bohr atom:
( m)
b) Red laser pointer:
(5 mW power,
2.5 mm beam radius)
Answer:
V/m
= 255

## Slide 37: Forces inside a solid
1. Let’s model an electron inside a solid.
2. Let’s displace the electron.
3. Find the restoring force.
5. If the displacement is small:
constant k

## Slide 38: Linear model
Restoring force + Applied force = ma
If the applied force is DC
If the applied force is AC
-
+
-
+
-
+
P > 0
(We get a small constant electron displacement).
Observations:
is proportional to
Refractive index depends on frequency

## Slide 39: What if you have both DC and AC fields?
-
+
-
+
-
+
P > 0
Restoring force + Applied force = ma
External voltage
Light
Solution:
Observation: Refractive index does not depend on , but k may be direction-dependent.
(a DC field just shifts the graph)

## Slide 40: Electron movement and refractive index
Refractive index depends on:
average atomic separation
frequency
density of dipoles
“Lorentz Oscillator Model”
nonlinear
optics
linear
optics
Light intensity
DC field strength
Restoring force + Applied force = ma
External voltage
Light
Solution:

## Slide 41: Electrically changing the refractive index
Thermo-optically
  In silicon, the change is of index near room temperature is 1.86 × 10-4 /K
Carrier injection
  In silicon, for light at 1.55 m wavelength, if Ne=Nh=1018 cm-3, then Δn = -1.1 × 10-3 and  = 14.5 cm-1.
  Optical loss is impossible to eliminate.
Kerr effect (apply a voltage)
  In silicon, Δn = 10-4 at a field of 1000 kV/cm = 100 V/m
Pockels effect (apply a voltage to a nonlinear material)
  Not available in silicon or any other centrosymmetric crystal
  In lithium niobate, Δn = 10-4 at a field of 6.3 V/m = 62.6 kV/cm
  (63 V/m is needed to get a Δn = 10-3)
  It’s fast.

## Slide 42: A more realistic potential
Linear model
Orbital model
Towards proton
Away from
proton

## Slide 43
Temperature dependence of lattice constants in LN
References, compiled by Minghao Shang, Ph.D. student
[1] Journal of Physics and Chemistry of Solids, 1966, 27(6-7): 1019-1026.
[2] IEEE International Conference on Oxide Materials for Electronic Engineering (OMEE). IEEE, 2012: 147-148.
[3] Journal of Crystal Growth, 1976, 33(1): 199-202.
[4] Materials, 2022, 15(13): 4716.
[5] L. Moretti et al., “Temperature dependence of the thermo-optic coefficient of lithium niobate, from 300 to 515 K in the
visible and infrared regions,” J. Appl. Phys. 98(3), 036101 (2005).

## Slide 44
Solution
Path 1
Path 2
Combined field
+
Example 3 (thermo-optics): In lithium niobate, TM light from a single laser at  = 1.55 m is split and follows two paths, each 1 mm long, and then the light recombines. One path is at room temperature (300 K). How much must the second path be heated if the light will recombine with destructive interference?

## Slide 45: Thermo-Optic Mach-Zehnder interferometer
G. Chen et al., “Integrated thermally tuned mach-zehnder interferometer in Z-cut lithium niobate thin film,” IEEE Photonics
Technol. Lett. 33(13), 664–667 (2021).
Tuning efficiency = 0.59 nm/V

## Slide 46
G. Chen, H.-L. Lin and A. J. Danner, "Highly Efficient Thermal Tuning Interferometer in Lithium Niobate Thin Film Using Air Bridge," IEEE Photonics J., vol. 13, no. 3, pp. 1-9, 2021.
Thermo-Optic Mach-Zehnder interferometer with air bridges

## Slide 47: Pockels effect in lithium niobate
Apply a DC field in the z-direction:
where r13=8.6 pm/V, r33=30.8 pm/V, r22 = r51 = 3.4 pm/V, r61 = -r22, n0=2.238 and ne=2.159.
r33
affecting z-polarization
An applied field along z
Apply a DC field in the x-direction:
General case:

## Slide 48: Z-cut modulator
G. Chen, H. -L. Lin, J. D. Ng and A. J. Danner, "Integrated Electro-Optic Modulator in Z-Cut Lithium Niobate Thin Film With Vertical Structure," IEEE Photonics Technol. Lett., vol. 33, no. 23, pp. 1285-1288, 2021.

## Slide 49
Example 4: A DC field is applied to barium titanate, a 4mm crystal with r13 = r23 = 19.5 pm/V, r33 = 97 pm/V, r42 = r51 =1640 pm/V. no = 2.488 ne = 2.424. Find .

## Slide 50: What other crystals give diagonal elements?
jk | 
xx or 11 | 1
yy or 22 | 2
zz or 33 | 3
yz, zy, 23 or 32 | 4
xz, zx, 13 or 31 | 5
xy, yx, 12 or 21 | 6

## Slide 51: What other crystals give diagonal elements?
jk | 
xx or 11 | 1
yy or 22 | 2
zz or 33 | 3
yz, zy, 23 or 32 | 4
xz, zx, 13 or 31 | 5
xy, yx, 12 or 21 | 6

## Slide 52: NUS Solar Quadcopter Team (2018)
https://www.youtube.com/watch?v=bJPplmWb-vI