## Slide 1: Lithium Niobate on Insulator Integrated Photonics from Fabrication to Classical and Quantum Applications
Presenter: Aaron Danner
National University of Singapore
E-mail: adanner@nus.edu.sg
Les Houches School of Physics, France, May 12, 2025 - May 23, 2025
Ecole de Physique des Houches 149 Chemin de la Côte F-74310 Les Houches
Part 1: How LN’s structure leads to its optical properties (Thurs, May 15, 10:45 am – 12:15 pm)
Part 2: Comparison of LN to other materials
(Fri, May 16, 10:45 am – 12:15 pm)

## Slide 2
If you have many randomly oriented sub-wavelength lithium niobate domains, what will happen optically?
There will be an effective refractive index (the macroscopic crystal now appears isotropic)
The Pockels effect disappears (because now we have inversion symmetry)

## Slide 3: Lithium niobate publication counting
Chart: "Thin film lithium niobate" publications
| 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023 | 2024 | 2025
 | 8 | 10 | 12 | 15 | 13 | 16 | 15 | 24 | 21 | 35 | 48 | 79 | 111 | 158 | 239 | 385 | 637 | 1080 | 1400 | 1830 | 932
[2] Jun Deng, Sajid Hussain, Vanga Sudheer Kumar, Wei Jia, Ching Eng Png, Lim Soon Thor, Andrew A. Bettiol, and Aaron J. Danner, "Modeling and experimental investigations of Fano resonances in free-standing LiNbO3 photonic crystal slabs," Opt. Express 21, 3243-3252 (2013)
[3] Deng Jun, Jia Wei, Ching Eng Png, Si Guangyuan, Jaesung Son, Hyunsoo Yang, Aaron J. Danner; Deep anisotropic LiNbO3 etching with SF6/Ar inductively coupled plasmas. Journal of Vacuum Science & Technology B 1 January 2012; 30 (1): 011208. https://doi.org/10.1116/1.3674282
[1] J. Deng, G. Si and A. J. Danner, "Dry etching of LiNbO3 using inductively coupled plasma," 2010 Photonics Global Conference, Orchard, Singapore, 2010, pp. 1-5, doi: 10.1109/PGC.2010.5706006.
First
try at NUS

## Slide 4
Lithium niobate etching in 2010

## Slide 5
Better etching
2010
2013
2018
[2] Jun Deng, Sajid Hussain, Vanga Sudheer Kumar, Wei Jia, Ching Eng Png, Lim Soon Thor, Andrew A. Bettiol, and Aaron J. Danner, "Modeling and experimental investigations of Fano resonances in free-standing LiNbO3 photonic crystal slabs," Opt. Express 21, 3243-3252 (2013)
[3] S. Y. Siew, E. J. H. Cheung, H. Liang, A. Bettiol, N. Toyoda, B. Alshehri, E. Dogheche, and A. J. Danner, “Ultra-low loss ridge waveguides on lithium niobate via argon ion milling and gas clustered ion beam smoothening,” Opt. Express, vol. 26, no. 4, pp. 4421–4430, Feb. 2018.
[1] J. Deng, G. Si and A. J. Danner, "Dry etching of LiNbO3 using inductively coupled plasma," 2010 Photonics Global Conference, Orchard, Singapore, 2010, pp. 1-5, doi: 10.1109/PGC.2010.5706006.

## Slide 6: Applications
01
Advanced Photonics 4.3 (2022): 034003.

## Slide 7
Thin film lithium niobate devices in our lab
Waveguide
Cross-section
Air bridge
1 by 2 MMI
4 by 4 MMI
Photonic crystal
Z-cut modulator

## Slide 8
8-inch wafer-level TFLN fabrication process and PDK development
Photonics heterogeneous integration of TFLN modulator on silicon photonics platform through die-to-wafer (D2W) bonding.
8-inch Thin-Film Lithium Niobate Platform
– Towards extremely high-speed modulators
Contact: Dr. Xianshu Luo, Luo_Xianshu@ime.a-star.edu.sg

## Slide 9: Lithium niobate compared to other materials

## Slide 10
Pockels Coefficients for Various Material Systems [updated, April 2025]
104
103
102
101
100
Pockels Coefficient [pm/V]
SiO2
GaAs
BBO
ZnTe
CdTe
ZnO
PbTiO3
KDP
KDA
DKDP
ADP
LiTaO3
LiNbO3
KTP
KTA
MNA
PZT
Polymers
SPCD
KNbO3
PLZT
BTO
SBN
KTN
Material
Chart made by Wang Zexian, Ph.D. student

## Slide 11
A. Petraru et al., ‘’Integrated optical Mach–Zehnder modulator based on polycrystalline BaTiO3.’’ Opt. Lett. 28,2527 (2003)
reff = 22 pm/V
r13 = 18 pm/V, r33= 23 pm/V
Leroy, F. et al. Guided-wave electro-optic characterization of BaTiO3 thin lms using prism coupling technique Opt. Lett. 38, 1037–1039 (2013).
Encouraging Early Results in Literature: Polycrystals of Barium Titanate (BTO)
Bulk BTO
Structural phase transition at 120°C can crack the crystal in fabrication processes such as etching or baking
The ion diffusion method which is used in lithium niobate modulator fabrication may not be possible for BTO
Key Challenge:

## Slide 12
FWHM > 0.36
L. Beckers et al., ‘’Structural and optical characterization of epitaxial waveguiding BaTiO3 thin films on MgO’’ Journal of Applied Physics 83, 3305 (1998)
Desired region
Historical Perspective: BTO on MgO
Multi-domain
BTO/MgO
B. Wessels, ‘‘Ferroelectric Epitaxial Thin Films for Integrated Optics.’’ Annu. Rev. Mater. Res. 37, 659–79 (2007)
A. Petraru, ‘’Optical and electro-optical properties of BaTiO3 thin films and Mach-Zehnder waveguide modulators’’, PHD Thesis. Universitat zu Koln (2003)
D. H. Kim and H. S. Kwok, ’’Pulsed laser deposition of BaTiO3 thin films and their optical properties’’ Appl. Phys. Lett. 67, 1803 (1995)
FWHM
= 0.6
MgO has a relatively small lattice mismatch of 5% and a low refractive index of 1.71.
r42=110 pm/V
FWHM=0.8097
Il-Doo Kim, ‘’Ridge waveguide using highly oriented BaTiO3 thin films for electro-optic application’’ Journal of Asian Ceramic Societies 2, 231–234 (2014)
FWHM =
0.45
Notes: MgO have a relatively small lattice mismatch with BTO. Normally BTO electro- optic modulators are fabricated on MgO. However, MgO has comparably large lattice mismatch with BTO and MgO is hydrophilous thus having a poor surface. Therefore BTO either grow a-c domains or single crystals but orientation wide spread.

## Slide 13
Reported Barium Titanate (BTO) modulators and structures
Low index substrate
BTO thin film
Such as MgO , SiO2 , …
To provide vertical confinement
Thin film BTO
= 900 pm/V
Largest r reported in thin film
a-c domain structure
S. Abel, Nature Materials 18(1), 42–47 (2019).
Felix Eltes et al., J. of Lightwave Tech., Vol. 37, No. 5 (2019)
Notes: This is really large r value achieved for multi-domain BTO thin film.

## Slide 14
PsiQuantum’s BTO device
PsiQuantum team. A manufacturable platform for photonic quantum computing. Nature (2025). https://doi.org/10.1038/s41586-025-08820-7

## Slide 15
A. Petraru et al., ‘’Integrated optical Mach–Zehnder modulator based on polycrystalline BaTiO3,’’ Opt. Lett. 28,2527 (2003)
Leroy, F. et al. “Guided-wave electro-optic characterization of BaTiO3 thin films using prism coupling technique,” Opt. Lett. 38, 1037–1039 (2013)
L. Beckers et al., ‘’Structural and optical characterization of epitaxial waveguiding BaTiO3 thin films on MgO,’’ Journal of Applied Physics 83, 3305 (1998)
Il-Doo Kim, ‘’Ridge waveguide using highly oriented BaTiO3 thin films for electro-optic application,’’ Journal of Asian Ceramic Societies 2, 231–234 (2014)
B. Wessels, ‘‘Ferroelectric Epitaxial Thin Films for Integrated Optics,’’ Annu. Rev. Mater. Res. 37, 659–79 (2007)
M. Yashima et al., “Size effect on the crystal structure of barium titanate nanoparticles,” J. Appl. Phys., 98(1), 14313 (2005)
P. Girouard, “χ(2) Modulator With 40-GHz Modulation Utilizing BaTiO3 Photonic Crystal Waveguides,” IEEE J. Quantum Electron., 53(4), 1–10, (2017)
S. Abel, "Large Pockels effect in micro- and nanostructured barium titanate integrated on silicon," Nature Materials 18(1), 42–47 (2019).
Barium Titanate (BTO) single crystal properties
x y z
= 8 pm/V
=
= 105 pm /V
= 1300 pm/V
Bulk BTO
BaTiO3 crystal
x
y
z
Thin film BTO on low-index insulator
Small lattice mismatch
Vertical mode confinement
Advanced Materials, 33 (37), 2101128 (2021)
λ = 1550 nm

## Slide 16
Plasma plume for BTO growth
Pulsed laser deposition (PLD)
10 mm
1. BTO thin film on DSO substrate
Growth
Good lattice match
Smaller refractive index
Substrate choice
Material | Refractive index
BaTiO3 | ~2.2
DyScO3 | ~2

## Slide 17
AFM morphology of BTO surface of 600 nm BTO/DSO with small rms roughness of 746.2 pm.
High quality single crystal BTO (001) and flat surface achieved at thicknesses required for optical modes.
XRD 2θ-ω coupled scan shows a single orientation of BTO (001), with c-axis out of plane.
XRD Δω scan at BTO (002) shows highly oriented film, with FWHM of 0.075o, indicating high crystal quality.
AFM morphology of BTO surface of 600 nm BTO/DSO with small rms roughness of 746.2 pm.
c axis oriented out of plane
Notes: We know that rough surfaces scatters lights out from the waveguides, causing a lot of loss. Therefore, a smooth surface would be necessary. With the thickness of 600 nm of BTO films, the surface maintains flat and the AFM image show a small rms roughness of less than 1 nm.
XRD 2θ-ω coupled scan shows that c-axis BTO single orientation, no other orientation out of plane is observed.
XRD Rocking curve scan show the distribution of c-orientation, FWHM of 0.075o at the BTO (002) indicates high crystal quality.
The XRD data comes from the fabricated device, it reflects our fabrication process did not lower the crystal quality.
(FYI, rocking curve FWHM at (001) is not comparable, and is normally half of it at (002).)

## Slide 18
Thin film BTO on DSO
No structural phase transition observed at up to 700°C
Bulk BTO
Helium-ion microscope picture of a well-etched sample surface
Advanced Materials, 33 (37), 2101128 (2021)
Hysteresis
Increased Tc and High temperature phase stability
Coercive field = 496 kV/cm
Notes: Volume V = a*b*c

## Slide 19
Pockels matrix of BTO thin film grown on DyScO3 (DSO) substrate
x y z
= 4.2 pm/V
= 4.6 pm /V
= 9.0 pm/V
Electric field is applied along the z direction
Refractive index change with DC voltage applied (λ = 636.6 nm)
Degraded crystal quality compared with BTO on DSO
Optical Materials Express, 13(1), 152-160 (2023)
Sample: IBSD

## Slide 20
Applied Physics Letters, 122, 031106 (2023)
Large Pockels coefficient r51 (r42) in BTO on insulator
x y z
= 600 pm/V
Theory: Off diagonal Pockels coefficients can rotate the optic axis
An active polarization rotator
With TE input
With TM input
With TE input
Experiment (a maximum power conversion of ~30%)
Simulated
26.1 dB

## Slide 21: Typical Waveguide Fabrication Procedure
Extracted r42 = 1268 pm/V

## Slide 22
Metal diffusion
Proton beam
Crystallinity control
Engineering refractive index contrast without dry etching BTO
Y. Cao et al., “Engineering refractive index contrast in thin film barium titanate-on-insulator,” Nano Letters, vol. 23, 16 (2023).
(Metal diffusion like in LN is possible)
1000°C for 10 h in Ar/H2
RMS=0.2 nm
RMS=13.4 nm
Mo diffused
BTO
1 µm
BTO
Diffused
Diffused
DSO
Air
w
h
w=0.5 µm
h = 250 nm
TM
λ = 532 nm

## Slide 23
Metal diffusion
Proton beam
Crystallinity control
Engineering refractive index contrast without dry etching BTO
Proton beam irradiation
Large Area Proton Beam (H+)
Crystallinity control
Y. Cao et al., “Engineering refractive index contrast in thin film barium titanate-on-insulator,” Nano Letters, Accepted (2023)

## Slide 24: Optical computing with Lithium Niobate

## Slide 25
phase shift
phase shift
FDTD simulation for illustration
A 2-port interferometer
Matrix-vector multiplication using optics
E1
E2
Reck, M., et al., Experimental realization of any discrete unitary operator. Physical Review Letters, 1994. 73(1): p. 58-61.
Clements, W.R., et al., Optimal design for universal multiport interferometers. Optica, 2016. 3(12): p. 1460.
Xu, X.-Y., et al., A Reconfigurable Photonic Processor for NP-complete Problems. arXiv preprint arXiv:2308.14156, 2023.
unitary
matrix
vector
product
For example, if =
For example, if =
45

## Slide 26
Functional Block
Arbitrarily large matrices are possible
phase shift
phase shift
2 x 2 optical matrix multiplier
2 x 2
2 x 2
2 x 2
2 x 2
Functional Block
3 x 3 optical matrix multiplier
3 x 3
Notes: After explaining the 2by2 interferometer, let’s move to the 3x3 condition. If we put three 2by2 interferometer in this way, we will get the 3x3 interferometer. And this structure could represent any unitary matrix.
Some additional structure is added to make up the difference of optical speed at different part of structure.
Total length is about 100 microns. For a 0.5cmx0.5cm wafer, 90x90 interferometer might be realized.

## Slide 27
Input 1
Input 2
Input 3
Output 1
Output 2
Output 3
Example: 3 x 3 matrix multiplication
Notes: Finite-Difference Time-Domain method
Then I did Lumerical simulation for this structure to verify the theory.

## Slide 28
Input 1
Input 2
Input 3
Output 1
Output 2
Output 3
Example: 3 x 3 matrix multiplication
Notes: Finite-Difference Time-Domain method
Then I did Lumerical simulation for this structure to verify the theory.

## Slide 29
1 mm
Scalability and speed
In lithium niobate,
For a 100 x 100 matrix,
If N x N increases to (N+1) x (N+1), then
The calculation time increases by
(SPEED IS LINEAR WITH N)
The chip area increases by 2N
All-to-all connectivity is maintained
How can we handle
non-unitary matrices?
any
matrix
unitary
matrix
unitary
matrix
diagonal
matrix
(singular value decomposition)

## Slide 30
SP
SP
SP
AM
AM
AM
AM
PM
PM
PM
PM
SP
SP
AM
Amplitude Modulator
PM
Phase Modulator (EO)
Waveguide
SP
SP
S
G
G
SP
1-by-2 50:50 MMI or y-branch
MZI
AM
MZI
AM
SP
SP
SP
SP
Port 1
Port 6
Port 2
Port 3
Port 4
Port 5
Chip-based 2x2 design

## Slide 31
Silicon photonics matrix-vector multiplier
Modulation Speed: limited to kHz
Footprint: 1.65 mm2
PD
MZI
Thermo-Optic Modulator
1x2 MMI
Laser Input
MZI
2x2 MMI
Zoomed
in

## Slide 32
SP
SP
SP
MZI
MZI
Lithium niobate version
Collaborator: Fabricated by Prof. Ya Cheng, East China Normal University

## Slide 33
Nonlinear Operation: Periodical Poling on Lithium Niobate Nanophotonic Waveguide
[1] X. Shi, D. Zhu, et al. "Efficient photon-pair generation in layer-poled lithium niobate nanophotonic waveguides." Light: Science & Applications 13.1 (2024): 282.
[2] F. Fu, et al., arxiv.org/abs/2504.18145
Pump Depleted SHG [1]
Resemblance to Sigmoid Curve [2]
Experimental
b
Ideal
50 μm
Fabricated by
Zhu Di, NUS

## Slide 34
Optical Neural Network Architecture
Optical Computing Verification I
Results

## Slide 35: Ising Machines

## Slide 36
What is an Ising computer ?
We seek a physical system which naturally tends to reach the lowest energy state.
Task: Minimize with
Quantum Annealing
Machine Learning and Computer Science
Healthcare &
Medicine
Optimisation
Financial Modelling
What problems do an Ising computer solve?

## Slide 37
“+1” set
“-1” set
“+1” set
“-1” set
“+1” set
“-1” set
“+1” set
“-1” set

## Slide 38
Simulations based on algorithm in:
Böhm, F., Verschaffelt, G. & Van der Sande, G. A poor man’s coherent Ising machine based on opto-electronic feedback systems for solving optimization problems. Nat Commun 10, 3538 (2019). https://doi.org/10.1038/s41467-019-11484-3
What does an Ising computer do physically?
+1
-1
(time)
A 100-bit annealer
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
1 1 1 1 1 1 1 1 1 1
We seek a physical system which naturally tends to reach the lowest energy state.
Task: Minimize with
(our group’s simulations)

## Slide 39
Examples of excellent existing Ising computers
https://www.fujitsu.com/global/services/business-services/digital-annealer/
https://www.dwavequantum.com/

## Slide 40: Non-photonic Ising machines
Memristors Crossbar-Matrix-Multiply Unit
Nat. Electron. 3. (2020):409
Scalable CMOS Ising Machine
IEEE Journal of Solid-State Circuits 57.3 (2022): 858
Stochastic Magnetic Tunnel Junctions Based P-Bit Circuit
Nature 573. (2019): 390
Optoelectronic Parametric Oscillator (OEPO)
Light: Science & Applications, 11.1 (2020): 333
Quantum Annealer
(D-Wave)
Nature Physics 10.3 (2014): 218
48-node All-to-All CMOS Ising Machine
Nat. Electron. 6.10 (2023):771
Results
Outlook
Introduction
Chip Design
Notes: Ising machine is widely studied and constructed on various physical system.

## Slide 41: Photonic Ising machines
Results
Outlook
Introduction
Chip Design
Free Space OPO
Nat. Photo. 8. 12 (2014):937
Fiber Optics OPO
Science 354.6312 (2016): 614
Opto-electronic oscillator
Nat. Com. 10.1 (2019): 3538
Integrated MZI
Optica 7.5 (2020): 551
Integrated OPOs on LN
arXiv: 2405.17355 (2024)
All-Optical Interferometer-Based Ising Machine
Manuscript accepted by Optica
Integrated MZI
Nature 640.8058 (2025): 361
Integrated OPOs on SiN
Nat. Com. 11.1 (2020): 4119
Additional Reference:
Applied Physics Reviews 11.4 (2024)
Notes: In the photonic area, it is also widely studied like……
For more photonic Ising machines, we recently published a review about them for your reference.

## Slide 42: Working Principle
[1] Böhm, F., Verschaffelt, G. & Van der Sande, G. Nat Commun 10, 3538 (2019).
[2] Lan et al., 5, 2400004 (2024).
(alternative optical algorithms are available too)
Purpose: Realize Ising Machine in Optical Domain
(equation 1) Photodetection
Linear operation (equation 2) MZI
For example, with three spins:
Matrix Multiplication
Nonlinear Operation
(1)
(2)
&

## Slide 43: Free Space All-Optical Ising Machine
Matrix Multiplication
Nonlinear operation

## Slide 44
1024 Spins (Square Lattice)
100 Spins (Square Lattice)
x10
x10
Experimentally solving a 1024-spin square lattice
To be published (Optica)
Notes: Iteration Speed per round: 0.6 second

## Slide 45
Footprint: 2 m2
10 ns optical calculation speed (per iteration), but 0.6 s including I/O
Photographs of the Ising Machine in action

## Slide 46: 50,000-spin problem solving (silicon chip)
x222
x222
49,284 Spin Problem
Comparing to simulated annealing running on advanced CPU: Intel Core i9-13900k
Over 440 iterations: 212x better solution
Both running for 150 mins: 9x better solution
Notes: These 50,000 spins are places as a 222x222 arrays. Each spin has a antiferromagnetic interaction with its four neighbours.
The graph in the middle illustrate the energy landscape of our system. Where we can it start from a random state, and gradually reach 97 percent of the global minimum.
If we compare the efficiency, both in 440 iteations, we reached 200x lower energy.
If we compare the speed, in 150 mins, we also reach 9 times lower energy.

## Slide 47: Solving MAXCUT problems
47
CUT Score of SPINIC (gnp-k4-100)
CUT Score of SPINIC (reg-4-100)
CUT Score of SA (gnp-k4-100)
CUT Score of SA (reg-4-100)
Low density graph: Able to outperform Simulated Annealing
High density graph:
Similar solution quality
as Simulated Annealing
(Hamlib dataset)
SA: Starting at 100 and cooling 1% per iteration
Notes: We also solve two 100-node MAXCUT problems with different complexity.

## Slide 48: Perspective among the best Ising machines
Category | Type | Key Component | Footprint | Maximum Experimental Spin Count | All-to-All Connection
CMOS Annealing Processor [1] | Electronics | SRAM | 23.65 mm2 | 30k | No
CMOS Chip Based Ising Machine [2] | Electronics | Oscillator | 1.8 mm2 | 48 | Yes
Quantum Photonic Microprocessor [3] | Integrated Photonics | MZI | 15 mm2 | 16 | …
Nanophotonic Parametric Oscillators [4] | Integrated Photonics | OPO | … | 70 | Yes
Coherent Ising Machine [5] | Fiber Optics | OPO | … | 100k | Yes
This Work | Integrated Photonics | MZI | 1.65 mm2 | 50k | Yes
References:
[1]: IEEE Journal of Solid-State Circuits 55, 145-156 (2020)
[2]: Nat. Electron. 6, 771-778 (2023)
[3]: Laser & Photonics Review 18, 2300304 (2024)
[4]: arXiv.2405.17355 (2024)
[5]: Sci. Adv. 7, eabh0952 (2021)
Notes: Here is a table comparing our system with the best ising machines, no matter it is cmos or photonic based. Specifically, our system has the smallest reported footprint since we need a 2x2 MZI only. Meanwhile, we have the second best experimental spin count due to our great scability. The only one beat us is a fiber-optics based ising machine and they use a 5km fiber, but we are a small photonic chip. Comparing with the ising chip, we have the most spin count.

## Slide 49: FPGA based test scheme
Results
Outlook
Introduction
Chip Design
Data Process and Storage
Probe
LN
chip
Fiber array
Electrodes
PD
PD
PD
PD
Zmod ADC
A/D
Laser Source
1550 nm
D/A
Pmod DAC (<1 kHz)
(high-bandwidth SZG connector)
(ZYNQ 7020 series * 2)
Zmod DAC (>1 MHz)
Packaged LN Chip
PD
FPGA
Amplifiers

## Slide 50
From pump-depleted SHG to Ising machine
Optical Computing Verification II
Cubic Lattice Ising Model
: nonlinear coupling coefficient
: propagation distance
: self-feedback strength
: coupling coefficient
Ising System
: pump power → Spin Amplitude
W. Fu, A. Danner, et al. "An Evolutionary Ising Optimization Framework for Unconstrained Binary Quadratic Programming" IEEE Transactions on Evolutionary Computation (2025).

## Slide 51
Acknowledgements
Funding:
Singapore National Research Foundation (NRF-CRP24-2020-0003)
We are looking for postdocs
adanner@nus.edu.sg
http://www.youtube.com/@adanner
https://danner.group